UNIT 17-18 LIFFORD WAY

BINLEY INDUSTRIAL ESTATE

COVENTRY CV3 2RN

TEL: 024 7623 3933   FAX: 024 7623 3928

E-mail: info@coventry-grinders.co.uk

Visit our site, www.coventry-grinders.co.uk

Company Reg no. 3129960 VAT Reg no. 487 623 115

Metric Key Steel Tolerances

Square Section

3mm square - 6mm square +.000 -.03mm

8mm square - 10mm square +.000 - .036mm

12mm square - 18mm square +.000 - .043mm

20mm square - 24mm square +.000 -.052mm

25mm square - 28mm square +.000 - .062mm

30mm square - 40mm square +.000 - .076mm

45mm square - 50mm square +.000 -.090mm

Flat Section

8mm x 7mm - 10mm x 8mm Width +000 - .036mm Thickness +.000 - .090mm

12mm x 8mm - 16mm x 10mm Width +.000 -.043mm Thickenss +.000 -.090mm

18mm x 11mm - 25mm x 14mm Width +.000 - .052mm Thickness +.000 -0.11mm

32mm x 18mm - 36mm x 20mm Width +.000 - .062mm Thickness + 0.11mm

40mm x 22mm - 50mm x 28mm Width +.000 - .062mm Thickness +.000 - 0.13mm

56mm x 32mm Width +.000 - .074mm Thickness +.000 - 0.16mm